Foreword

SAC/TC 243 is in charge of this English translation. In case of any doubt about the contents of English translation, the Chinese original shall be considered authoritative.

This standard is drafted in accordance with the rules given by GB/T 1.1-2009.

This standard replaces YS/T 275-2008 (high purity aluminium) in whole.

In addition to a number of editorial changes, the following technical deviations have been made with respect to the YS/T 275-2008:

——Revised standard name (see standard cover, 2008 edition cover);

——Revised the scope of application (see 1 in the 2008 Edition);

——Revised of normative reference documents (see 2, 2 in the 2008 Edition );

——The Al99.9999 designation has been added and the designation requirements have been revised (see article 3.1 in the 3.1 2008 Edition).

——Revised chemical composition (see 3.2, Notes in Table 1 of 2008 edition).

——Added uranium, thorium, vanadium and boron (see 3.2) in the chemical composition of Al99.999.

——Added vanadium and boron in the chemical composition of Al99.999 designation.

——Revised the appearance quality requirements (see 3.3 in the 2008 Edition);

——Revised ingot shape requirements (see 3.4 in the 2008 Edition);

——Increased other requirements (see 3.5);

——Revised chemical composition analysis method (see 4.1 in the 2008 edition);

——Added arbitration analysis method (see 4.1 in the 2008 edition);

——Revised inspection and acceptance requirements (see 5.1 in the 2008 edition );

——Increased weight requirements (see 5.4)

——Revised sampling and sample preparation requirements (see 5.5.1.1,the 2008 edition of 5.4.1.1);

——Revised arbitration sampling requirements (see 5.5.1.2,the 2008 edition of 5.4.1.3);

——Revised the judgement of inspection results (see 5.6,the 2008 edition of 5.5);

——Revised requirements for marks, packaging, transportation, storage and certification of quality (see 6, 2008 Edition 6);

——Revised contents of the order (or contract) (see 7 in the 2008 edition).

This standard was proposed and prepared by national nonferrous metals Standardization Technical Committee(SAC/TC 243).

This standard is issued by: Xinjiang joinworld Co.,Ltd.

The main translators of this standard are: Ma Lin, Feng Wei, Li Yongqi, Ma Xiaohong. Song Yuping,

The previous editions of YS/T 275-2008 are as follows:

——GB/T 8179-1987;

——YS/T 275-1994, YS/T 275-2000, YS/T 275-2008.

High purity Aluminium ingot

1.Scope

This standard specifies the requirements, test methods, inspection rules, marks, packaging, transportation, storage and quality certificates, orders (or contracts) of high purity aluminium ingot.

This standard is applicable to high purity aluminium ingot produced by segregation melting (step crystallization, direct solidification purify, zone melting) or electrochemical refining (electrolysis) with Al 99.99% or above as raw material.

2.	Normative references

The following referenced documents are indispensable for the application of this document. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

GB/T 3199 Wrought aluminium and aluminium alloy products-Packing, marking, transporting and storing

GB/T 8170 Rules of rounding off for numerical values & expression and judgement of limiting values

GB/T 25820 Steel strips for packing

YS/T 244 Chemical analysis methods of high purity aluminum(all parts)

YS/T 870 Chemical analysis of high purity aluminium. Determination of trace impurities. Inductively coupled plasma mass spectrometry

YS/T 871 Chemical analysis of high purity aluminium-Determination of trace impurities－Glow discharge mass spectrometry

QB/T 3811 Plastic packing belt.

3．Requirement

3.1 Product classification

According to chemical composition, the high purity aluminium  ingot is divided into three grades, Al99.9999, Al99.9995 and Al99.999.

3.2 Chemical composition

The chemical composition of high purity aluminium  ingot should meet the requirements of Table 1. If the purchaser has requirements for heavy metal elements such as arsenic, cadmium, mercury or other impurities, the contents shall be determined by the supplier and the purchaser after consultation and specified in the order (or contract).

Table 1

| Designation | Purity code | Chemical composition (mass fraction) |
| --- | --- | --- |
|  |  | ≤，μg/g | Al content≥，% |
|  |  | Si | Fe | Cu | Zn | Ti | Ga | Pb | Cd | Ag | In | Th | U | V | B | Other Individuala |  |
| Al99.9999 | 6N | 0.2 | 0.2 | 0.1 | 0.1 | 0.1 | 0.1 | 0.2 | 0.1 | 0.1 | 0.2 | ＜0.0005 | ＜0.0005 | 0.1 | 0.1 | 0.1 | 99.9999b |
| Al99.9995 | 5N5 | 1.0 | 1.0 | 0.5 | 0.9 | 0.5 | 0.5 | 0.5 | 0.2 | 0.2 | 0.2 | ＜0.005 | ＜0.005 | 1.0 | 0.5 | 0.2 | 99.9995b |
| Al99.999 | 5N | 2.5 | 2.5 | 1.0 | 0.9 | 1.0 | 0.5 | 0.5 | 0.2 | 0.2 | 0.2 | - | - | 1.0 | 1.0 | 0.5 | 99.999c |
| Note: High purity metal as main material to produce high purity aluminium or purity aluminium alloy in the field of microelectronics, should be accordance with the GB / T33912. a.Others each means the elements that are not listed or not specified in the table. b.The mass fraction of aluminum is the difference between 100% and total content of all elements not less than 0.000005%. The values of all elements should be expressed as 0.0000XX% before summation and 0.0000X% after summation. c.The mass fraction of aluminum is the difference between 100% and total content of all elements not less than 0.00001%. The values of all elements should be expressed as 0.000XX% before summation and 0.000X% after summation. |

3.3 Appearance quality

The surface of the fine aluminum ingot should be clean, without severe flash, allowing slight slag inclusions.

3.4 Ingot weight and ingot type

3.4.1 The weight of each batch or each refined aluminum ingot is determined by the supplier and the purchaser.

3.4.2 Ingots should be suitable for packaging, transportation and storage needs.

3.5 Other requirements

When the purchaser has special requirements for the quality of the product, the supplier and the purchaser shall decide through consultation and indicate them in the order or contract.

4. Test method

4.1 Chemical composition

4.1.1 Conventional chemical analysis is performed only for elements with numerical values specified outside the "Al" and "each other" columns in Table 1.

4.1.2 For Al99.9999, Al99.9995 and Al99.999 grades, chemical composition analysis is carried out in accordance with YS/T 870, YS/T 871, YS/T 244 (all parts) or the method agreed by both suppliers and purchasers. The arbitration analysis shall be conducted according to the provisions of YS/T 871 or by consultation between the supplier and the purchaser.

4.1.3 The analysis value is judged by Revised comparison method. The numerical reduction rules are carried out according to the relevant provisions of GB / T 8170. The reductions are consistent with the limit digits in Table 1.

4.2 Appearance quality

The appearance quality of high purity aluminium  ingot is visually inspected.

5 Inspection rule

5.1 Inspection and acceptance

5.1.1 The product shall be inspected by the supplier to ensure that the quality of the product meets the requirements of this standard and the order (or contract), and to fill it in the quality certificate.

5.1.2 The purchaser shall inspect the received products in according to the requirements of this standard. If the inspection result is not in conformity with this standard and the provisions of the order (or contract), it shall be submitted to the supplier in written form and settled through consultation between the supplier and the purchaser. Objections of chemical composition and other properties shall be raised within one month from the date of receipt of the product, and objections of other properties shall be raised within three months from the date of receipt of the product. If arbitration is required, the organization authorized by the supplier and the purchaser shall be entrusted to do so and sampled together by both parties.

5.2 Batches

The products should be submitted for acceptance in batches, and each batch should be made up of the same furnace.

5.3 Weight counting

The product should be weighed.

5.4 Inspection project

Each batch of refined aluminum ingots should be inspected for chemical composition and appearance quality.

5.5 Sampling and sample preparation

5.5.1 Chemical composition

5.5.1.1 Melt sampling and sample preparation

The melt sampling should be carried out in the ingot flow groove by graphite spoon, the sampling mold should be pre-heated and impurities are not available. Sampling should be taken out in the beginning of the casting and the end of the casting. Samples can also be cut off from the refined ingots, each sample should be at least three specimens. The specimens should have no porosity, slag, loose and crack.

5.5.1.2 Sampling arbitral

A piece of refined aluminium ingot is taken from any batch, in the position of upper, middle and bottom. If the upper, middle and bottom position is not clear, at least three pieces of random samples should be prepared. Sampling by cutting method, grind away at least 2mm thickness for GDMS test. The sample preparation should be accordance with the GDMS requirement.

5.5.2 Appearance quality

The appearance quality should be checked by each ingot.

5.6 Judgement of inspection

5.6.1 If the chemical composition of any sample is not qualified, the batch shall be rejected.

5.6.2 When the appearance quality of any refined aluminum ingot is not qualified, it is judged this ingot is not qualified.

6 Marking, packaging, transportation, storage and certificate of quality

6.1 Marking

6.1.1 Product marking

Each batch of aluminum ingots should be cast or printed with the factory sign and melting number.

6.1.2 Package marking

Each bundle of aluminium ingots shall be stuck at least two labels (or certificate) with vibrant, waterproof and not easy to fall off. The follow content should be indicated in the label:

a）product name;

b) designation;

c) smelting number;

d) net weight;

e) number of blocks;

f) date of production;

g）the seal of the supplier's quality inspection department. (or the signature or seal of the quality inspector).

6.2 Packaging

6.2.1 Refined aluminium ingot should be baled as "#" or other forms.

6.2.2 Aluminum ingots can be bundled with steel strips, high strength plastic wrapping strips or other materials, but it should be guaranteed the aluminum ingots stable.

6.2.3 Steel strips for bundling shall be rust-proof and in conformity with GB/T 25820. Plastic wrapping strips for bundling shall be in accordance with QB/T 3811 or be negotiated between suppliers and purchasers.

6.3 Transportation and storage

The transportation and storage sites of refined aluminum ingot should be clean, in accordance with the requirements of GB/T 3199 or negotiated between suppliers and purchasers.

6.4 Certificate of quality

Product quality certificate should be attached on each batch of products and state:

a) supplier name;

b) product name;

c) the designation name;

d) batch number;

e) net weight and pieces;

f) test result and the seal of the supplier's quality inspection department. .

g) the standard number;

h) packaging date (or ex-factory date).

7 Purchase order (or contract) content

The purchase order (or contract) that orders products listed in this standard should include the following items::

a) product name;

b) the designation name;

c) ingots type and ingots weight;

d) quality;

e) any other requirement not list in this standard should negotiated by supplier and purchaser (including chemical composition, ingot weight and ingot type, test method, marking, packaging, transportation and storage) .

f) this standard number.

# Text boxes

Issued by

Ministry of industry and information technology of the People’s Republic of China

YS

Implementation date: 2018-09-01

Issued date:2018-04-30

High purity aluminium ingot

高纯铝锭

(English Translation)

YS/T 275-2018

Replace YS/T 275-2008

People's Republic of China nonferrous metals industry standard

ICS 77.120.10

H 61