| ICS 77.150 H 64 | YS |
| --- | --- |

Nonferrous Metals Industry Standard of the People's Republic of China

YS/T 261—2011

Replace YS/T 261—1994

Spodumene concentrate

锂辉石精矿

（English Translation）

| Issue date:2011-12-20 | Implementation date:2012-07-01 |
| --- | --- |

Issued by  Ministry of Industry and Information Technology of the People's Republic of China

Foreword

SAC/TC243 is in charge of this English translation.In case of any doubt about the contents of English translation, the Chinese original shall  be considered authoritative.

This standard replaces the YS/T 261—1994 Spodumene concentrate.

The following technical deviations have been made with respect to the  YS/T 261—1994:

—Modified the grade and chemical composition of spodumene concentrate;

—Modified the granularity requirements of spodumene concentrate.

This standard was proposed and prepared by SAC/TC243 National Nonferrous Metals Standardization Technical Committee.

The previous editions of this standard are as follows:

—YS/T 261—1994.

Spodumene concentrate

1  Scope

This standard specifies the requirements, testing methods, inspection, marking, packaging, transportation, storage and quality certificate as well as contract/order content for spodumene concentrate.

This standard is applicable to spodumene concentrate obtained using various  mineral processing. The spodumene concentrate is widely used in glass ceramic industry and producing various chemical products of lithium.

2  Normative Reference

The following referenced documents are indispensable for the application of this document. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

YS/T 509.1,Methods for chemical analysis of spodumene and lepidolite concentrates—Determination of lithium oxide,sodium oxide and potassium oxide contents—Flame atomic absorption spectometric method

YS/T 509.5,Methods for chemical analysis of spodumene and lepidolite concentrates—Determination of ferric oxide content—O-phenanthroline photometric method and EDTA compleximetric method

YS/T509.6,Methods for chemical analysis of spodumene and lepidolite concentrates—Determination of phosphorus pentoxide content—The molybdenum blue photometric method

YS/T509.8,Methods for chemical analysis of spodumene and lepidolite concentrates—Determination of calcium oxide and magnesium oxide content—Flame atomic absorption spectrometric method

YS/T509.10,Methods for chemical analysis of spodumene and lepidolite concentrates—Determination of manganous oxide content —Persulfate oxidation photometric method

3  Requirements

3.1  Product classification

The product is divided into six grades according to the applied field and chemical composition.

3.2  Chemical composition

Chemical composition of the product shall conform to Table 1.

Table 1

| Grade | Li2O not less than /% | Impurity not more than/% |  |  |  |  | Recommended application |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Fe2O3 | MnO | MgO | Na2O+K2O | P2O5 |  |
| Microlite grade-1 | 7.50 | 0.15 | 0.10 | ― | 1.0 | 0.5 | Mainly used for producing glass ceramics and glaze of high-grade ceramics |
| Microlite grade-2 | 7.00 | 0.30 | 0.15 | ― | 1.5 | 0.5 |  |
| Ceramics grade | 6.50 | 0.60 | 0.25 | 一 | 1.8 | 0.5 | Mainly used for producing ceramics |
| Chemical grade-1 | 6.00 | 2.5 | 0.40 | 0.20 | 2.00 | 0.5 | Mainly used for producing chemical products of lithium |
| Chemical grade-2 | 5.50 | 2.8 | 0.50 | 0.30 | 3.00 | 0.5 |  |
| Glass grade | 5.00 | 0.25 | 0.15 | 一 | 3.00 | 0.5 | Mainly used for producing glass |

3.3  Granularity

Granularity shall be mutually agreed by the supplier and purchaser.

3.4  Moisture content

Moisture content of the product shall not be more than 8%.

3.5  Appearance quality

The product shall not contain  impurities that could be seen.

4  Test methods

4.1  Chemical composition analysis of the product shall be carried out in accordance with YS/T 509.1,YS/T 509.5, YS/T 509.6, YS/T 509.8 and YS/T 509.10.

4.2  The determination method of granularity shall be mutually agreed by the supplier and purchaser.

4.3 The determination of the moisture content is carried out  by gravimetric method: weight 200 g specimen, place it into oven at 105℃, dry for 2h; weight it and calculate the moisture content.

4.4  Examination of appearance  shall be carried out by visual inspection.

5  Conformity with this standard

5.1 Inspection and acceptance

5.1.1 The product shall be inspected by the 	Quality Control Department of the supplier to ensure the quality conforming to this standard and contract/order and the quality certificate should also be offered.

5.1.2 The purchaser shall inspect the received product according to  this standard.If the inspection results are found not in conformity to this standard, the purchaser shall inform the supplier within one month from the date of  receiving the product,and negotiate with the supplier. If any arbitration is needed, sampling shall be carried out by both parties at the purchaser’s site.

5.2 Lots

The product shall be delivered for inspection and acceptance in lots. Each lot shall consist of products of the same grade of product, with  the weight of not more than 3000 t for chemical usage,  other usage’s weight  shall not exceed 60 t.

5.3 Inspection items

Inspection items and sample  numbers for each lot shall be as specified in Table 2.

Table 2

| Inspection items | Sample numbers and specification | Chapter number for the requirements | Chapter number for the test method |
| --- | --- | --- | --- |
| Chemical composition | follow 5.4 | 3.2 | 4.1 |
| Granularity |  | 3.3 | 4.2 |
| Moisture content |  | 3.4 | 4.3 |
| Appearance quality |  | 3.5 | 4.4 |

5.4 Sampling and preparation

5.4.1 Each lot shall be evenly sampled by inserting a tube (plastic or stainless steel tube).

5.4.2 For bagged concentrate of the same grade, if each lot is more than 10 t, 10% of the total number of bags shall be selected; if each lot is less than 10 t, 20% of the total number of bags shall be selected. Open all the bags selected and insert a tube in each of them to take samples not less than 2000 g; mix the samples evenly, reduce them to about 500 g and divide  them into three parts, take 200 g for chemical analysis; the sample for chemical analysis needs to be milled to  less than 0.074 μm.

5.4.3 For bulk concentrate, samples shall be taken in quincunx form and then prepared according to 5.4.2.

5.5 Determination of inspection results

5.5.1 If the result of chemical composition analysis fails the inspection, then double samples shall be taken for retesting; if there is still any inspection result that fails, then this lot is judged as unqualified.

5.5.2 If granularity inspection fails, this lot of product is judged as unqualified.

5.5.3 If moisture content inspection fails, this lot is judged as unqualified.

5.5.4 If appearance quality inspection fails,  this lot is judged as unqualified.

6  Packaging, marking, transportation, storage and quality certificate

6.1 Packing, transportation and storage

The product may be packed in bags or bulk, depending on the purchaser's requirement and shall be protected from rain during transport and storage.

6.2 Marking

6.2.1  If the product is packed in bags, then each bag shall indicate:

a) Supplier name;

b) Product name and grade;

c) Lot number;

d) Trademark.

6.2.2 If the product is shipped in bulk, a form containing the items under 6.2.1 can be completed and handed over to the purchaser.

6.3 Quality certificate

Quality certificat shall be attached to each lot of the product,which indicates:

- Supplier name, address, phone and fax numbers;

- Product name and grade;

- Lot number;

- Net weight and number of bags;

- Analysis and inspection results, and stamp of the Quality Control Department;

- Number of this standard;

- Release date.

7  Contract (or order) contents

The contract (or order)  contents for the product listed in this standard shall include the following contents:

- Product name;

- Grade;

- Quantity;

- Number of this standard;

e) Other information.

_______________