06

Foreword

SAC/TC 243 is in charge of this English translation.In case of any doubt about the contents of English translation,the Chinese original shall be considered authoritative.

The standard is drafted in accordance with the rules given in the GB/T 1.1-2009.

This standard was proposed by the China Nonferrous Metals Industry Association.

This standard was prepared by SAC/TC 243 (National Technical Committee for Standardization of Nonferrous Metals).

The previous editions of this standard are as follows:

Magnesium Alloy Forgings for Aerospace

Scope

This standard specifies the requirements, test methods, inspection rules and marking, packaging, transportation, storage， quality certificates and order forms (or contracts) of magnesium alloy forgings for aerospace.

This standard is applicable tothe magnesium alloys for aerospace in the form of die forgings and free forgings (hereinafter referred to as forgings).

Normative references

The following referenced documents are indispensable for the application of this document. For dated references, only the edition clted applies. For undated references, the latest edition of the referenced document(including any amendments)applies.

GB/T 231.1, Metallic materials - Brinell hardness test - part 1 test method

GB/T 4297, Inspection method for macrostructure of wrought magnesium alloy products

GB/T 5153, Designation and composition of wrought magnesium and magnesium alloys

GB/T 6519, Ultrasonic inspection of wrought aluminium and magnesium alloy products

GB/T 8170, Rules of rounding off for numerical values & expression and judgement of limiting values

GB/T 13748(all part), Chemical analysis methods of magnesium and magnesium alloys

GB/T 16865, Test pieces and method for tensile test for wrought aluminium and magnesium alloys products

GB/T 32792, Packing, marking, transporting and storing of magnesium alloy wrought products

Requirements

Product Classification

Designation, temper, specification, class(level比较好) and code

The designation, temper, specification and class of forgings shall conform to the requirements in Table 1. The forging code shall be determined by the supplier and the purchaser through negotiation. Other designations or tempers needed shall be determined by both parties through negotiation and indicated in the order form (or contract).

Table 1 Designation, temper, specification and class

| Designation | Temper | Specification a | Class b |
| --- | --- | --- | --- |
| AZ40M、AZ41M、ME20M | H112 | — | ClassⅡ,ClassⅢ |
| AZ61M | O | — | ClassⅡ,ClassⅢ |
| AZ80M | T4 | — | ClassⅡ,ClassⅢ |
| ZK61M | T5 | Piece Weight≤30 Kg and Max.thickness≤100 mm | ClassⅡ,ClassⅢ |
| VW83M | T6 | — | ClassⅡ |
| aThe shape and size of forgings shall be determined by drawing or contract signed by both sides. b Forgings are classified into ClassⅡ and Class Ⅲ. Different levels of forgings have different requirements, such as metallic compound segregation et al.. Specific level shall be indicated in the contract according to the application circumstances by purchaser. |

Marking and examples

The marking of proudcts is  expressed in the order of product name, this standard serial number, designaiton, temper, code (dimension) and class. Examples are expressed as follows:

Example 1：

An order for the ClassⅡ, die forging, designation of AZ40M, temper of H112, and code of K12, is as follows:

Die Forging GB/T XXXX-AZ40MH112-K12-ClassⅡ

Example 2：

An order for the ClassⅡI , free forging, designation of ZK61M, temper of T5, and dimension of Φ 650 mm × 80 mm (height) , is as followsi:

Free Forging GB/T XXXX-ZK61MT5-Φ650×80-ClassⅢ

Chemical Composition

The chemical composition of forgings shall be in accordance with GB/T 5153.

Dimensional Deviation

The dimensional deviation of forgings shall conform to the requirements of drawings or contracts signed by both parties.

Mechanical properties

The tensile properties at room temperature shall be as specified in Table 2.

Table 2 Tensile properties at room temperature and Brinell Hardness

| Alloy | Temper | Die Forgings or Free Forgings | Longitudinal | Transversal | Brinell hardness HBW |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Tensile Strength Rm MPa | Elongation After Fracture A % | Tensile Strength Rm MPa | Elongation After Fracture A % |  |
|  |  |  | No Less Than |
| AZ40M | H112 | All | 235 | 5.0 | - | - | 45 |
| AZ41M | H112 | All | 235 | 5.0 | - | - | 45 |
| AZ61Mc | O | All | 255 | 8.0 | - | - | 50 |
| AZ80M | T4 | All | 265 | 6.0 | - | - | 55 |
| ME20M | H112 | All | 215 | 8.0 | - | - | 45 |
| ZK61Ma | T5 | Die Forgings | 295 | 8.0 | 265 | 6.0 | 60 |
|  |  | Free Forgings | 275 | 6.0 | 255 | 5.0 |  |
| VW83M | T6 | Die Forgings | 390 | 6.0 | - | - | - |
|  |  | Free Forgings | 370 | 5.0 | - | - |  |
| a Mechanical properties of ZK61M alloy die forgings and free forgings with a piece weight of more than 30 Kg and a quenching thickness of more than 100 mm shall be separately agreed by both parties.(中文标准里没有) |

Brinell Hardness

The Brinell hardness of forgings shall be as specified in Table 2.

Macrostructure

Defects such as porosity, crack, non - metallic inclusion and flux slag inclusion are not permitted in the macrostructure of forgings.

The flow direction of forgings shall conform to the requirements as specified in the drawing. When there is no indication in the drawing, the flow direction shall be distributed along the direction of the maximum external dimension, and no obvious cutting is permitted. Passage（Cross Flow） and severe eddy(Vortex Flow) are not permitted in die forgings.

Defects of oxide film in macrostructure shall be as specified in Table 3.

The segregation of manganese compounds in the AZ40M, AZ41M, AZ61M, AZ80M and ME20M alloys shall be as specified in Table 4.

The segregation of metal compounds in ZK61M and VW83M alloys shall be as specified in Table 5.

Table 3 Oxide film

| Class | Macrostructure | Fracture |
| --- | --- | --- |
|  | TestedArea c mm2 | Oxide filma | TestedArea c mm2 | Oxide filmb |
|  |  | Points | Length Per Point mm |  | Total Area mm2 | Area Per Point mm2 |
| Ⅱ、Ⅲ | 1×105 | ≤5 | ≤2 | 1×104 | ≤9 | ≤3 |
| aThe length of the oxide film on the macrostructure test shall be not less than 0.3 mm. bThe stripe-like defect of the oxide film on the fracture test shall be counted in terms of length. The allowable value of the oxide film shall be in accordance with the requirements in this Table. cThe tested area refers to the sum of all tested areas of the same forging. The tested area smaller than the specified area shall also be calculated based on the latter one. If the tested area is larger than the specified area, the points of defects shall be calculated proportionally and the defect length per point shall be no change.与中文标准不同 |

Table 4 Segregation of manganese compounds

| Class | Segregation of Manganese Compounds |
| --- | --- |
|  | Macrostructure | Fracture |
|  | Testeda Area mm2 | Total Area mm2 | Area Per Point mm2 | TestedArea a mm2 | Total Area mm2 | Area Per Point mm2 |
| Ⅱ | 1×105 | ≤10 | ≤4 | 1×104 | ≤10 | ≤4 |
| Ⅲ |  | ≤13 | ≤5 |  | ≤13 | ≤5 |
| aThe area tested refers to the sum of all tested areas of the same forging. The tested area smaller than the specified area shall also be calculated based on the latter one. If the tested area is larger, then the points of defects shall be calculated proportionally and the length per point shall not change. 同上 |

Table 5 Segregation of metallic compounds

| Class | Segregation of Metal Compounds |
| --- | --- |
|  | Macrostructure | Fracture |
|  | TestedArea a mm2 | Total Area mm2 | Area Per Point mm2 | TestedArea a mm2 | Total Area mm2 | Area Per Point mm2 |
| Ⅱ | 1×105 | ≤6 | ≤2 | 1×104 | ≤6 | ≤2 |
| Ⅲ |  | ≤9 | ≤3 |  | ≤9 | ≤3 |
| aThe area tested refers to the sum of all tested areas of the same forging. The tested area smaller than the specified area shall also be calculated based on the latter one. If the tested area is larger, then the points of defects shall be calculated proportionally and the length per point shall not change. 同上 |

Fractural Microstructure

The oxide film on the fractural microstructure of forgings shall be as specified inTable 3.

The fluxed slag inclusion and the compounds segregation defects more than those specified in Table 4 and Table 5 shall not be permitted in the fractural microstructure of forgings.

Ultrasonic Inspection

If the ultrasonic inspection is required for forgings, it shall be determined by both parties through negotiation and indicated in the order form (or contract).

Appearance

The forging surface shall be smooth and clean. Oxidation treatment shall be done on the finished forging surface,, neither exposing the base metal nor exfoliating. Oil protection shall be done after oxidation treatment.

Crack and folding on the forging surface to be machined shall be removed. Peeling, bubbling, bruising, pressing and other defects are permitted to inspection and cleaning in to obtain the defects’ depth.. One half of the nominal machining allowance shall be guaranteed for forgings, no matter the defects removed or not removed.

Folding, peeling, bruising, rough scar and other defects are not permitted on the non-processed surface of die forgings, but the existing defects is permitted to remove by the supplier. The removal part shall be rounded off and the one-side limit size shall be ensured for die forgings.

Test Methods

Chemical Composition

Arbitration analysis of chemical composition of forgings shall be conducted in accordance with GB/T 13748.

The analysis value shall be determined by the modification comparison method, and the value shall be modified in accordance with the relevant provisions of GB/T 8170, and the modified digit shall be consistent with the limit digit as specified in GB/T 5153.

Dimensional Deviation

The external dimensions of free forgings shall be measured by calipers, steel gauge, tape measure or measuring instruments with corresponding accuracy.

The dimensions and deviations of die forgings shall be measured by the marking method, special sample gauge or measuring instruments with corresponding accuracy.

Mechanical Properties

The tensile test at room temperature shall be conducted in accordance with GB/T 16865.

Brinell Hardness

The Brinell Hardness test shall be conducted in accordance with GB/T 231.1.

Macrostructure

The macrostructure test shall be conducted in accordance with GB/T 4297.

Fractural microstructure

The fractural microstructure test shall be conducted in accordance with GB/T 4297.

Ultrasonic Inspection

The ultrasonic inspection shall be conducted in accordance with GB/T 6519.

Appearance

The appearance shall be inspected visually. When the defect depth cannot be  determined, it can be measured by the grinding method.

INSPECTION RULES Inspection rules

      - Inspection and acceptance

      - The products shall be inspected by the supplier to ensure that the product quality of the products conforms to the requirements of this standard and the order form (or contract), and the quality certificate shall be filled in.

      - The purchaser shall inspect the received products in accordance with the provisions of this standard. If the inspection results are not in conformity with the provisions of this standard and the order form (or contract), they shall be submitted to the supplier in writing form, and decision shall be done through consultation between the supplier and the purchaser Objections that belonging to the surface quality or external dimensions shall be filed within one month from the date of receiving the products. Objections that belonging to other natures shall be filed within three months from the date of receiving the products. If arbitration is needed, it can be conducted by an organization approved by both sides, and samples shall be taken by supplier.

Batch

      - The products shall be submitted for acceptance in batches. Each batch shall consist of the same designation, the same melting, the same temper, the same specification and level. The weight of each batch is not limited.

      - If the forgings are of large volume and the same melting product cannot be batched, the way of batching shall be determined by both parties through negotiation and indicated in the order form (or contract).

Inspection Items

      - Chemical composition, dimensional deviation, mechanical properties, Brinell hardness, macrostructure, fractural microstructure and appearance inspections shall be carried out on each batch of forgings.

      - If the forging product requires ultrasonic inspection, inspection rules shall be negotiated by both parties.

Sampling

The sampling of the inspection items shall conform to the requirements in Table 6.

Table 6 Sampling

| Inspection Items | Sampling Rules | Requirement Clauses | Inspection Clauses |
| --- | --- | --- | --- |
| Chemical Composition | 1 Sample per Melting or Batch | 3.2 | 4.1 |
| Dimensional Deviation | 1 Sample per Piece | 3.3 | 4.2 |
| Mechanical Properties at Room Temperature | 2 Samples per Piece 1 Piece per Batch (Heat Treatment Furnace) | 3.4 | 4.3 |
| Brinell Hardness | 2 Samples per Piece 1 Piece per Batch (Heat Treatment Furnace) | 3.5 | 4.4 |
| Macrostructure | 1 Piece per Batch | 3.6 | 4.5 |
| Fractural MicrosStructure | 1 Piece per Batch | 3.7 | 4.6 |
| Ultrosonic Inspection | 1 Sample per Piece | 3.8 | 4.7 |
| Appearance | 1 Sample per Piece | 3.9 | 4.8 |

Determination of Inspection Results

      - When the  chemical composition of any sample is unqualified, the batch (or melting) is unqualified.

      - When the dimensional deviation of any forging is unqualified, the forging is unqualified.

      - When the tensile properties at room temperature of any sample are unqualified, reinspection shall be taken with double quantity of samples cut from adjacent parts of the sample or from another forging. If all of  reinspection results are qualified, the batch (furnace) of products are qualified. If any of samples is still unqualified, the batch (furnace) of products is unqualified. The qualified pieces can be delivered to the purchaser if each piece is inspected by the supplier as agreed upon by both parties.

      - If Brinell Hardness of any sample is unqualified, it is allowed to cut double quantity of samples from adjacent parts of the sample or from another forging for reinspection. If the reinspection results are all qualified, the batch (holding) of products are determined qualified. If certain sample is still unqualified, the batch (holding) of products are determined unqualified. The qualified pieces can be delivered to the buyer if each piece is inspected by the supplier as agreed upon by both parties. 同上

      - When  the macrostructure of any sample is unqualified , it shall be determined as follows:

  - The batch shall be scrapped due to porosity, crack, non-metallic inclusion, flux inclusion slag, oxide film and metallic compound segregation.

  - If the macrostructure streamline is different from that of the standard sample, or if the eddy current (Cross Flow) and the cross current (Vortex Flow) exist, reinspction is permitted to taken with double quantity of samples in the same batch by the supplier. The batch is qualified if the reinspection of samples is qualified . If any of samples is still unqualified, the batch of products is unqualified.

When the fractural microstructure of any sample is unqualified, the batch (or melting) is unqualified

When the ultrasonic inspection  of any forging is unqualified , the forging is unqualified.

When the appearance of any forging is unqualified, the forging is unqualified.

- Marking, packaging, transportation, storage and quality certificate

The container marking of forgings shall be in accordance withGB/T 32792.

Each accepted forging shall be stamped at the specified position with the following mark:

- Inspection  stamp of the supplier's technical supervision department;

- Alloy designation;

- Supply temper;

- Forging code;

- Melting number;

- Batch number.

The packaging, transportation and storage of forgings shall be in accordance with GB/T 32792.

Quality Certificate

- Quality certificate shall be provided for each batch of forgings, which includes as follows: Supplier name;

- Product name;

- Alloy designation;

- Supply temper;

- Specification;

- classLevel;

- Melting number;

- Batch number;

- Net weight or piece(s);

- Inspection results of each item;

- Packaging date;

- C;

- Inspection stamp of the supplier's technical supervision department.

- Order form (or contract)The order form (or contract) of the forgings using this standard shall include as follows Product name;

- Alloy designation;

- Supply temper;

- Specification;

- classLevel;

- Weight or piece(s);

- V;

- Requirement for ultrasonic inspection;

- Other requirements.

# Text boxes

Issued by

General Administration of Quality Supervision, Inspection and Quarantine of the People's Republic of China

Standardization Administration of the People’s Republic of China

Implemented date: ××-××-××××

Issued date: ××-××-××××

格式不对

Magnesium Alloy Forgings for Aerospace

Draft for Review

National Standard of the People's Republic of China

ICS 77.150.10

H61

GB/T 37596—2019