ICS 77.150.99

H68

Industry Standard of Nonferrous Metals of the People's Republic of China

YS/T 943-2013

Palladium(II) sulfate

硫酸钯

(English Translation)

Issue date: 2013-10-17

Implementation date: 2014-03-01

Issued by Ministry of Industry and Information Technology of the People's                  Republic of China

Foreword

Sac/TC 243 is in charge of this English translation. In case of any doubt the contents of English translation, the Chinese original shall be considered authoritative.

This standard is drafted in accordance with the rules given in the GB/T 1.1-2009.

This standard was prepared by SAC/TC 243 Chinese Nonferrous Metal Standardization Technical Committee.

Palladium(II) sulfate

1  Scope

This standard specifies the requirements, test methods, inspection, marking, packaging, transportation, storage, quality certificate and the order (or contract) information of Palladium(II) sulfate.

This standard is applicable to Palladium(II) sulfate application in fine chemical and electroplating industry.

2  Normative references

The following referenced documents are indispensable for the application of this document. For data references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

GB/T 23276 Method for chemical analysis of palladium compound--Determination of palladium content--Complexometric titration using butanedione dioxime releasing EDTA.

YS/T 362 Determination of trace impurities in purity palladium by atomic emission spectrometric.

3  Requirements

3.1  Product classification

Products should be classified as anhydrous palladium sulfate and dihydrate palladium sulfate, Their chemical formulas are shown as follows:

Anhydrous palladium sulfate: PdSO4;

Palladium sulfate dihydrate: PdSO42H2O;

3.2  Chemical component

3.2.1  The mass fraction of palladium in anhydrous palladium sulfate should be≥ 52.0%.

The mass fraction of palladium in palladium sulfate dihydrate should be ≥ 44.0%.

3.2.2  The quantity of impurities in palladium sulfate should comply with the specification in table 1.

Table 1. The mass fraction of impurities in palladium sulfate (should not be higher than)                                                                         %

| Ag | Au | Pt | Rh | Ir | Pb | Ni | Cu | Fe | Cd | Cr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.001 | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 |

3.3  Dissolution test

The palladium sulfate should dissolve in dilute sulfuric acid completely.

3.4  Appearance

Anhydrous palladium sulfate should be dark red crystal.

Palladium sulfate dihydrate should be red brown crystal powder.

4  Test method

4.1  Determination of palladium

As specified in GB/T 23276, a certain amount of compound shall be measured to determine the quantity of palladium.

4.2  Determination of impurities

Weigh a certain amount of palladium compound which is accurate to 0.0001g and reduce the compound to metal palladium by heating in a stream of hydrogen, then determine the amount of impurities as specified in YS/T 362.

4.3  Dissolving test

Measure 0.5g sample and add 20 mL dilute sulfuric acid(1+3), The sample should dissolve in dilute sulfuric acid completely.

4.4  Appearance

Visual test method shall be applied to check the appearance of palladium sample.

5  Inspection method

5.1  Inspection and acceptance

5.1.1  The product should be inspected by the Quality Control Department of the supplier to ensure all products should be in conformity with this standard (or contract). A quality certificate shall be filled out accordingly.

5.1.2  Inspection of the product received shall be carried out by the purchaser in accordance with the requirements of this standard. In case of non-conformity with the requirements of this standard or the stipulation of the contract, complaints of non-conformity should be made within 15 days. In case of arbitration, sampling for arbitration shall be conducted by both parties with the demander.

5.2  Lots

Product should be checked in lot, and each lot should be produced from the same feed reaction.

5.3  Inspection item

For each lot of product, mass fraction of palladium, mass fraction of impurities, dilute sulfuric acid soluble test and visual appearance should be carried out before the delivery.

5.4  Sampling

5.4.1  Sampling for chemical content and solubility test: mix each group of products and take sample from different parts. The weight of each sample accounts 1-5% for total products and it should not be less than 10 g, then apply the quartation method to divide sample to requirement amount (samples should avoid being wet ).

5.4.2  The appearance of each bottle of product should be checked visually.

5.5  Judgment of test results

If the test results of palladium's mass fraction, appearance, impurities' mass fraction and dissolution test do not in conformity with this standard, the inspection lot which they represent shall be deemed not to comply with the requirement of this standard.

6  Marking，packaging, transportation, storage and quality certificate

6.1  Marking

6.1.1  Marking of product

The marking of inspection conformed product should include the following:

a)  Name of the provider;

b)  Name of the product;

c)  Production lot;

d)  The quantity of product;

e)  Date of manufacture.

6.2  Packaging, transportation and storage

6.2.1  Product should be packaged in polypropylene or polyethylene bottle and seal the  container well. All bottles should be put in wood or paper box and the packaging box should be filled with paper scrap or polyfoam as buffer to avoid being loose.

6.2.2  Product shall be transported by railway, highway or water way.

6.2.3  Product should be placed in dry environment and avoid being wet.

6.3  Quality certification

Each lot of product should be attached with quality certification which is followed by:

a)  Name, address, telephone and fax number of the provider;

b)  Name of the product;

c)  Batch number;

d)  Quantity;

e)  Inspection result for all content and signet of technical supervision department;

f)  Serial number of this standard;

g)  Date of production.

7.  Ordering (or contract) content

The order (or contract) for the products listed in this standard should contain the following information:

a)  Name of the products;

b)  The quantity of products;

c)  Serial number of this standard;

d)  Others.